Zhejiang Runhe Chemical New Material Co., Ltd

Add: Rm.1906, Guangli Mansion, No.136, Qingchun Road, Hangzhou, Zhejiang, China

Tel: +86-571-85092338   Fax: +86-571-87246635

Specification

【Product Name】Levelling Agent for Coating RH-T1045

【Component】Polyether modified polysiloxane

【Instruction】

Special modified Polysiloxane. It is excellent organosilicone surfactant auxiliary which can supply good wetting property of bottom materials and anti-cratering property. It increases the smoothness of surface, scratch resistance and anti-adhesive property, improves leveling,gloss, and prevents Bernard swirl. Applied as additives in solvent-based, solvent-free based and water-based paint system.

【Basic Character】

Appearance	: Colorless to amber transparent oily liquid

Non-volatile content:＞97.0%

Refractive Index(25ºC)：1.4300-1.4400

Viscosity(25ºC)：200-500cs

【Usage】

It can be added as original form or pre-dilution form. Dosage: 0.05%-1.0%

【Package】

200Kg, or 25Kg/Plastic barrel

【Storage】

Transportation as non-dangerous goods

Store in cool and ventilated warehouse. 12 months of storage period.