Zhejiang Runhe Chemical New Material Co., Ltd

Add: Rm.1906, Guangli Mansion, No.136, Qingchun Road, Hangzhou, Zhejiang, China

Tel: +86-571-85092338   Fax: +86-571-87246635

Specification

【Product Name】Levelling Agent for Coating RH-T1057

【Component】Polyether modified polysiloxane

【Instruction】

It has super wetting,smooth and anti-scratch properties.It  makes the paints and coatings clear and smooth,glossy.It will increase the scratch resistance.Good recoat properties.

Apply to solvent-based, solvent-free based and water-based system.

【Basic Character】

Appearance	:Colorless to amber transparent oily liquid

Viscosity:200-500cps

Reflexable index:1.430-1.440

【Usage】

RH-T1057is low dosage，good effect.The dosage is depended on the system,solvent,resin and total solid content.

The dosage of RH-T1057 is generally 0.5-1.0% of the coatins，it can added in the sand grind,formulation preparation,and the last process. It has different  characters in different systems. Before usage,a test is a necessary.

It will get cloudy in low temperature,that will disappear under heat,and it will not affect the product quality.

【Package】

180Kg, or 25Kg/Plastic barrel

【Storage】

Store in cool and ventilated warehouse. 12 months of storage period.